Rubberecycle

1985 Rutgers University Blvd.

Lakewood, NJ 08701

Toll Free	(888) 463-6846

Phone		(732) 363-0600

Fax		(732) 370-4247

Website	www.rubberecycle.com

E-mail		info@rubberecycle.com

Product Guide Specification

Specifier Notes:  This product guide specification is written according to the Construction Specifications Institute (CSI) 3-Part Format.

The section must be carefully reviewed and edited by the Architect to meet the requirements of the project and local building code.  Coordinate this section with other specification sections and the Drawings.

Delete all Specifier Notes when editing this section.

SECTION 02792

POURED-IN-PLACE SPRAYGROUND SURFACING

Specifier Notes: This section covers Rubberecycles “Aquabond®” resilient, poured-in-place, sprayground surfacing. Consult Rubberecycle for assistance in editing this section for the specific application.

PART 1	GENERAL

1.01	SUMMARY

A.	Section Includes: Poured-in-Place, Aquatic & Sprayground Surfacing: AquaBond

1.2	RELATED SECTIONS

Specifier Notes: Edit the following list of related sections as required. List other sections with work directly related to this section. Include the section number and title of the following two Division 2 sections, if they are referenced in this section.

A.	Section 02_______ - ____________________ :  Asphalt subsurface.

B.	Section 02791 - Playground Surfacing Tiles.

C.	Section 02880 - Play Field Equipment and Structures:  Playground equipment.

D.	Section 03300 - Cast-in-Place Concrete:  Concrete subsurface.

1.3	REFERENCES

Specifier Notes: List standards referenced in this section, complete with designations and titles. This article may be omitted when specifying manufacturer’s proprietary products and recommended installation.

A.	ASTM D 412 - Standard Test Methods for Vulcanized Rubber and Thermoplastic Elastomers--Tension.

B.	ASTM D 624 - Standard Test Method for Tear Strength of Conventional Vulcanized Rubber and Thermoplastic Elastomers.

C.	ASTM C 1028 - Standard Test Method for Determining the Static Coefficient of Friction of Ceramic Tile and Other Like Surfaces by the Horizontal Dynamometer Pull Meter Method.

D.	ASTM D 2859 - Standard Test Method for Ignition Characteristics of Finished Textile Floor Covering Materials.

E.      ASTM F 1551-03 – Standard Test Methods for Comprehensive Characterization of Synthetic Turf Playing Surfaces and Material: Suffix-DIN 18-035, Part 6: Water Permeability of Synthetic Turf Systems and Permeable Bases.

F.	US Consumer Product Safety Commission (CPSC) Handbook for Playground Safety.

1.4	SUBMITTALS

A.	Submit listed submittals in accordance with conditions of the contract and Division 1 submittal procedures section.

B.	Product Data:  Submit manufacturer's product data

C.	Verification Samples:  Submit manufacturer's samples of AquaBond Sprayround surfacing  of at least 2 inches by 3 inches.

D.	Test Reports:  Submit test reports from qualified independent testing agency indicating results of the following tests:

1. Tensile Strength: ASTM D 412

2. Elongation at Break:  ASTM D 624

3. Slip Resistance: ASTM C 1028

4. Fire Resistance: ASTM D2859

5. Permeability: ASTM 1551-03

E.	Certificate of Compliance:

1.      Submit manufacturer's certificate of compliance indicating materials comply with specified requirements.

2.       Submit certificate of qualifications of the sprayround surfacing installer

F.	Manufacturer's Project References:

1.	Submit list of successfully completed projects.

2.	Include project name, location, and name of owner’s representative.

G.	Installer's Project References:

1.	Submit list of successfully completed projects.

2.	Include project name, location, and name of owner’s representative.

H.	Maintenance Instructions:  Submit manufacturer's maintenance and cleaning instructions.

I.	Warranty:  Submit manufacturer's standard warranty.

1.5	QUALITY ASSURANCE

A.	Manufacturer's Qualifications:  Manufacturer shall meet a minimum of 1 of the following 2 requirements.

1.	Engaged in manufacturing of poured-in-place sprayground surfacing of similar type to that specified, with a minimum of 5 years successful experience.

2.	Furnished a minimum of 10,000 square feet of poured-in-place sprayground surfacing of similar type to that specified.

B.	Installer's Qualifications:

1.	Utilize an installer with successful experience in installation of poured-in-place sprayground surfacing of similar type to that specified.

2.	Employ persons trained for installation of poured-in-place sprayground surfacing.

3.	Certified by manufacturer

4.      Approved by manufacturer.

1.6	DELIVERY, STORAGE, AND HANDLING

- General:  Comply with Divison 1 Product Requirement Section.

- Delivery:  Deliver materials in manufacturer's original, unopened containers with original product identification labels.

C.	Storage and Protection:

1.	Store materials in accordance with manufacturer's instructions.

2.	Store materials in a dry area at a minimum temperature of 50 degrees F (10 degrees C) for a minimum of 72 hours before installation.

D.	Handling:  Protect materials during handling and installation from harmful environmental conditions.

1.7	PROJECT CONDITIONS

A.	Material Temperature:  Ensure material temperature is a minimum of 50 degrees F (10 degrees C) at time of installation.

B.	Air Temperature:  Install surfacing when ambient temperature is a minimum of 40 degrees F (4 degrees C) and a maximum of 90 degrees F (32 degrees C) for a minimum of 24 hours before, during, and after installation.

1.8	WARRANTY

- Project Warranty: Refer to conditions of the contract for project warranty provisions.

- Manufacturers Warranty:  Submit manufacturers standard warranty document.

- Materials and Workmanship:  AquaBond sprayground surfacing shall be warranted for defects in materials and workmanship for 2 years from date of completed installation.

PART 2	PRODUCTS

2.1	MANUFACTURER

A.	Rubberecycle LLC., 1985 Rutgers University Blvd, Lakewood, NJ 08701. Toll Free (888) 436-6846.  Phone (732) 363-0600.  Fax (732) 370-4247.  Website www.playgroundrubbermulch.com.  E-mail info@rubbermulch.com.

2.2	AQUABOND SPRAYGROUND SURFACING

A.	Poured-in-Place Sprayground Surfacing:  “AquaBond”.

1.	Description: Synthetic rubber sprayground surfacing consisting of a resilient, seamless poured-in-place surface.

2.	Material:  EPDM granules mixed with 100 percent solids MDI polyurethane binding agent

a.      Thickness: ½ inch

b.	Binder to Rubber Ratio:  21 percent.

c.	Compacted Density:  40 pcf.

Specifier Notes: Specify thickness of wear course.

d.	Thickness:  [1/2 inch]

Specifier Notes: Specify colors for poured-in-place sprayground surfacing. Multiple colors can be combined to create a speckled appearance. Consult Rubberecycle for availability of custom colors and for additional information.

8.	Colors:  [Black]  [Royal Blue]  [Light Blue] [Terra Cotta]  [Cocoa Brown] [Beige] [Yellow] [Orange] [Forest Green] ____________ ]  [As indicated on the Drawings].

Specifier Notes: Specify percent of colored granules in relation to percent of black granules.

1) 	Percent Color: [25 percent color, 75 percent black] [50 percent color, 50 percent black]                     [75 percent color, 75 percent black] [100 percent color 0 percent black]

B.	Test Results

1.	Minimum Static Coefficient of Friction, ASTM C 1028:

a.	Dry: 0.74

b.	Wet:  0.55

2.	Tensile Strength, ASTM D 412: 10 - 15 psi. Elongation: 10-15%

3.	Tear Strength, ASTM D 624:  4.5 pounds/force/inch

4.	Flammability, Burning Pill, ASTM D 2859:  Pass.

5.      Permeability, ASTM F 1551 -03, Part 6: 2200 inches/hour

PART 3	EXECUTION

Specifiers Notes: Specify actions required to determine that conditions are acceptable to receive products of the section.

3.1	EXAMINATION

- Site Verification of Conditions: Verify that substrate conditions are suitable for installation of poured-in-place sprayground surfacing.

- Verify that the appropriate sub-grade elevation has been established for the particular surface being installed.

- Verify that the subsurface has been installed per the architectural, site or equipment plans including accessibility and use zones. Notify Architect if areas are not acceptable.  Do not begin installation until unacceptable conditions have been corrected.

3.2	PREPARATION

A.	Prepare subsurface in accordance with manufacturer's instructions and recommendations

Specifier Notes: Specify subsurface of concrete, or asphalt. Due to the porosity of RubberBond playground surfacing, it is important that a proper subsurface drainage system be constructed.

Specifier Notes: Include the following paragraph when a concrete subsurface is required.

B.	Concrete Subsurface:

1.	Concrete subsurface shall be as specified in Section 03300.

2.	Apply light broom finish.

3.	Ensure concrete is sound with no cracks or loose material.

4.	Ensure concrete is a minimum of 14 days old.

5.      Ensure that all concrete curing compounds and any other contaminants have been removed

6.      Surface shall be dry and clean

Specifier Notes: Include the following paragraph when an asphalt subsurface is required.

C.	Asphalt Subsurface:

1.	Asphalt subsurface shall be as specified in Section 02_______ .

2.	Ensure asphalt is sound with no cracks or loose material.

3.	Ensure asphalt has cured for a minimum of 30 days

3.3	INSTALLATION

A.     Do not proceed with installation until all applicable site work, including substrate preparation, playground equipment installation and other relevant work has been completed.

B.	Install poured-in-place sprayground surfacing in accordance with manufacturer's instructions at locations indicated on the Drawings.

C.	Ensure prepared subsurface is dry and clean.

D.	Install edges in accordance with manufacturer's edge detail instructions and as indicated on the Drawings.

Specifier Notes: Installations over 1,500 square feet may contain a cold seam. Consult Rubberecycle for additional information.

E.	Install cold seams in areas containing graphics and as indicated on the Drawings.

3.4	CLEANING

A.	Clean poured-in-place playground safety surfacing in accordance with manufacturer's instructions.

3.5	PROTECTION

Specifier Notes: Estimated time for poured-in-place to cure will range from 12 to 48 hours depending on temperature and humidity. Consult Rubberecycle for additional information.

A.	Do not allow foot traffic until poured-in-place playground safety surfacing has cured.

B.	Protect completed playground safety surfacing from damage during construction and curing.

END OF SECTION